**0W-40 SN/CF DPF**

0W-40 is a blend of advanced technology components formulated to be fully compatible with the latest Diesel Particulate Filters (DPFs) and Gasoline Catalytic Converters (CATs). 0W-40 is designed to help provide superior performance and protection with potential fuel saving benefits.

**Certificates And Standards:**

API SN, API SL, API CF,

MB-Approval 229.31, MB-Approval 229.51, MB-Approval 229.52,

GM-LL-A-025,

ACEA C2, ACEA C3

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 150 |
| **Flash Point, °C** | ASTM D92 | Min. 220 |
| **Pour Point, °C** | ASTM D97 | Max. -40 |