**10W-40 SL/CF**

10W/40 is semi synthetic engine oil that produces to respond the lubrication need of modern high speed and high efficiency turbocharged engines by syn- thetic and high quality base oils and high-tech additives. It is used safely in all vehicles that work by gasoline, diesel and LPG. Provides fuel economy by excellent viscosity control property. Effective detergent and dispersant additives prevent deposit formation and keeps engine clean.

**Certificates And Standards:**

API SL/CF

VW 501.01 / 505.00

ACEA A3/B3-04

MAN M 3277

MB Approval 229.1

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear-Bright |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 130 |
| **Flash Point, °C** | ASTM D92 | Min. 225 |
| **Pour Point, °C** | ASTM D97 | Max. -30 |
|  |  |  |