**15W-40 SL/CF**

It is a gasoline engine oil produced by blending high quality base oils with high performance additives.

**Properties**

Makes the first work easy in the cold, makes effective lubrication at hot weather.

Protects the engine against all kinds of rust and corrosion and extends the life.

Excellent viscosity control feature allows the fuel economy.

Effective detergent and dispersant additives prevent deposit formation and keeps engine clean.

**Certificates And Standards:**

API SL/CF

VW 501.01 / 505.00

ACEA A3/B3-04

MB Approval 229.1

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear-Bright |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 110 |
| **Flash Point, °C** | ASTM D92 | Min. 200 |
| **Pour Point, °C** | ASTM D97 | Max. -24 |
|  |  |  |