**5W-20 SN/CF**

5W/20 is a full synthetic engine oil that is prepared by synthetic base oils and high-tech performance additive packets. It is suitable for all vehicles, work with gasoline and diesel.

**Properties**

It provides fuel economy and long service life by its excellent viscosity control feature.

It forms extra protection layer against to abrasion by bonding to surface of engines with smart molecules that contains and it does not lose performance at any conditions.

It makes easy to work at cold weather by its viscosity.

By the high viscosity index it has a high resistance to tearing.

It prevents the formation of residue, soot, varnish and deposit

**Certificates And Standards:**

API SN

ILSAC GF-5

FORD WSS-M2C948-B

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Values** |
| **Kinematic Viscosity (100°C) [mm2/s = cSt]** | ASTM D445 | 5,6-9,3 |
| **Viscosity Index** | ASTM D2270 | Min. 160 |
| **Flash Point, °C** | ASTM D92 | Min. 220 |
| **Pour Point, °C** | ASTM D97 | Max. -39 |