**15W-40 CF-4/SJ**

15W-40, is a high performance, low viscous and highly stabile diesel engine oil that can be used various applications. It fulfils requirements of diesel engines in wide application ranges during the year. It is general engine oil that is suitable to be used in fleets having high motor powers so as to carry heavy loads. It shows the best performance against abrasion, corrosion and residue formations. For this reason, it can be used in longer service ranges even under harsh environmental conditions. It is suitable to be used in any kind of turbo charge engine.

**Certificates And Standards:**

API CF-4/SJ,

ACEA A3/B4,

MB 228.3, MB 229.1,

MAN M3275,

Mack EO – M PLUS,

ALLISON C4,

Volvo VDS-3

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear-Bright |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 120 |
| **Flash Point, °C** | ASTM D92 | Min. 225 |
| **Pour Point, °C** | ASTM D97 | Max. -24 |
|  |  |  |