**5W-40 CI-4/SL**

5W/40 is a semi-synthetic motor oil enriched with a mixture of premium additives and premium base oils, especially for the conditions of use of light commercial diesel vehicles. It significantly reduces the negative effects caused by stop-start, sudden acceleration and braking or short-term use effects caused by long-term use at medium load and heavy city traffic. Provides fuel maintenance savings and minimizes the effects of overheating or cold starting. It keeps the performance at the highest level throughout the year by preventing the formation of harmful deposits in the engine oil.

**Certificates And Standards:**

CI-4/SL,

ACEA E3/B3/ B4,MB 228.3,

MAN M-3275,

Volvo Vds-2

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 130 |
| **Flash Point, °C** | ASTM D92 | Min. 220 |
| **Pour Point, °C** | ASTM D97 | Max. -35 |