**CUTTING OIL 32**

CUTTING OIL, is a qualified oil that is formulated with quality base oils obtained through modern refining processes. It exhibits extra resistance against high pressure in cutting, broaching, penetrating, grinding and scratching processes through Sulphur chloride it contains.

***Technical Specifications-32***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear &Bright |
| **Kinematic Viscosity (40°C), [cSt]** | ASTM D445 | 28,8-35,2 |
| **Viscosity Index** | ASTM D2270 | Min. 95 |
| **Flash Point, °C** | ASTM D92 | Min. 205 |
| **Pour Point, °C** | ASTM D97 | Max. -25 |
|  |  |  |