**ECOBENNZ 2T**

Is specially designed to provide high performance for use in motorcycles, go-karts and all other two stroke engines. It is used in air or water-cooled two-cycle engines, motorcycles, lawn mowers and agriculture tools. Use fuel/oil ratios as specified by the engine manufacturer up to a maximum of 50:1.

**Certificates And Standards:**

|  |  |
| --- | --- |
| API TC |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 7,5-11,3 |
| **Viscosity Index** | ASTM D2270 | Min. 110 |
| **Flash Point, °C** | ASTM D92 | Min. 210 |
| **Pour Point, °C** | ASTM D97 | Max. -12 |