**ECOBENNZ 4T 10W/40**

4T 10W-40 is synthetic 4-stroke motorcycle oil which blended with synthetic base oils and high quality additives for four-cycle, air- or water-cooled motor- cycles. This oil is wet-clutch compatible and recommended for motorcycles where an API SL or JASO MA/MA2 fluids are specified.

**Certificates And Standards:**

|  |  |  |  |
| --- | --- | --- | --- |
| API SL, JASO MA2 (T903:2011), JASO MB (T903:2011), JASO MA (T903:2011) |  |  |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 12,5-16,3 |
| **Viscosity Index** | ASTM D2270 | Min. 145 |
| **Flash Point, °C** | ASTM D92 | Min. 210 |
| **Pour Point, °C** | ASTM D97 | Max. -25 |