**75W-80 GL-5**

75W-80 SYN, Formulated synthetic base oils with new additive technology give improved lubrication and longer life for equipment. Suitable for automotive and heavy duty equipment transmission, axles, differentials where an EP (extreme pressure) lubricant is required when the manufacturer recommends a GL-5 transmission oil with a viscosity of SAE 75W-80.

**Certificates And Standards:**

|  |  |  |
| --- | --- | --- |
| API GL-5/GL-4, ZF TE-ML 05A, 7A, 12E, 16B, C and D, 17B, 19B, 21 B, MAN 342M-1, MAN 342 M-2, Scania STO 1273.12, DlN 51517 Part 3, U.S. Steel 224, AGMA 9005-D94 |  |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 8,4-13,5 |
| **Viscosity Index** | ASTM D2270 | Min. 130 |
| **Flash Point, °C** | ASTM D92 | Min. 210 |
| **Pour Point, °C** | ASTM D97 | Max. -39 |