**SAE 140 GL-1**

They are gear oils produced for use in automotive gearboxes operating at normal load and speed, where there is no excessive pressure, and where API GL-1 level oil is recommended. Use in gear cartridges, synchromesh gearboxes and differentials that do not require heavy load since they do not contain extreme pressure additives.

**Certificates And Standards:**

|  |  |  |
| --- | --- | --- |
| API GL-1 |  |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 24,0-32,5 |
| **Viscosity Index** | ASTM D2270 | Min. 92 |
| **Flash Point, °C** | ASTM D92 | Min. 245 |
| **Pour Point, °C** | ASTM D97 | Max. -10 |