**TRUCK FLUID 422**

TRUCK 422, is multi-purpose universal tractor transmission oil (UTTO) which is crafted with highly refined mineral base oils and additive packages. It can be used for agricultural and construction machines power transmission units, oil-bath brakes, hydraulics, gears, axles and other transmission systems. It shows very good performance in powertrain of moving equipment, drive axles, clutches and the PTO& hydraulic systems. High performance TRUCK 422 oil is suitable to use for diesel / gasoline engines (STOU).

**Certificates And Standards:**

|  |  |  |
| --- | --- | --- |
| API GL-4, CF/SF, SAE 80W, John Deere J20C, Massey Ferguson CMS M1143 and 1135, Case New Holland MAT 3525 and 3526, Allison C4, ZF TE-ML 07B, 06D, 06C, 06B, Ford M2C 134D |  |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 9,5-12,5 |
| **Viscosity Index** | ASTM D2270 | Min. 140 |
| **Flash Point, °C** | ASTM D92 | Min. 210 |
| **Pour Point, °C** | ASTM D97 | Max. -20 |