**TRUCK FLUID 426**

TRUCK 426, is an extra high performance multipurpose tractor oil designed to meet or exceed transmission and hydraulic oil requirements. The advanced technology in TRUCK 42-6 is designed to maximize the performance of agricultural and commercial tractors operating in a wide variety of environments and condi- tions. Heavy-duty transmissions, differentials, final drives, hydraulic systems, power steering systems, wet brakes, PTOs and hydrostatic drives and recommended in off-highway industries including: agriculture, construction, and quarrying.

**Certificates And Standards:**

|  |  |  |
| --- | --- | --- |
| API GL-4, CF-4 -FORD-ESEN, M2C 86B-MASSEY, FERGUSON, CMS M1135, VOLVO WB-101 |  |  |

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 9,7 |
| **Viscosity Index** | ASTM D2270 | Min. 145 |
| **Flash Point, °C** | ASTM D92 | Min. 220 |
| **Pour Point, °C** | ASTM D97 | Max. -36 |