**GRAFFIT CALCIUM GREASE**

GRAPHITE GREASE (CALCIUM), It is a black colored grease with calcium soap containing graphite prepared with mineral oils.

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method NLGI 00 NLGI 0 NLGI 1 NLGI 2 NLGI 3**  |  |
| **Color** |  Black |  |
| **Soap Type** | ASTM D2270 Calcium  |  |
| **Cone Penetration, worked, 0,1 mm, 25 °C /**  | ASTM D217 400-430 355-385 310-340 265-295 220-250 |  |
| **Dropping Point, °C** | ASTM D566 min 185 min 185 min 185 min 185 min 185 |  |