**LITHIUM GREASE**

Is lithium soap grease formulated with superior quality base oils and additives, used for a wide range of purposes in various industries. It is recommended for the wheel ball bearings and central lubrication systems of automobiles, commercial vehicles, sports utility vehicles agricultural machines and heavy duty machines not used at extremely heavy loads or extremely high temperatures. It can also be safely used in ball bearings of electric motors.

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method NLGI 0 NLGI 1 NLGI 2 NLGI 3**  |  |
| **Color** |  Yellow Brown |  |
| **Soap Type** | ASTM D2270 Lithium  |  |
| **Cone Penetration, worked, 0,1 mm, 25 °C /**  | ASTM D217 355-385 310-340 265-295 220-250 |  |
| **Dropping Point, °C** | ASTM D566 min 185 min 185 min 185 min 185 |  |