**MOLIBDEN LITHIUM GREASE**

Molybdenum lithium: Lithium Soap Industrial Grease is a gray-black lithium soap grease with molybdenum disulfide that reduces friction and wear.

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method NLGI 1 NLGI 2 NLGI 3** |  |
| **Color** | Yellow Brown |  |
| **Soap Type** | ASTM D2270 Lithium |  |
| **Cone Penetration, worked, 0,1 mm, 25 °C /** | ASTM D217 310-340 265-295 220-250 |  |
| **Dropping Point, °C** | ASTM D566 min 185 min 185 min 185 |  |